## Slide 1: Porous materials for trapping and detection of space contaminants
CCMPP-2023
Guillaume Rioland, Delphine Faye
CNES
September, 2023
guillaume.rioland@cnes.fr

## Slide 2: Table of contents
Introduction
Trapping
  Porous materials selection
  Shaping
Detection
  Porous materials selection
  Implementation
Conclusion
Porous materials for trapping and detection of space contaminants – CCMPP 2023

## Slide 3: Introduction
particulate contaminant
visible deposit of particles, fibers, chips…
(µm to a few mm)
mainly on ground
molecular contaminant
accumulation of monolayers (10 to 100 nm)
mainly in flight, sometimes on ground
Contaminant (ECSS-Q-ST-70-01): any unwanted molecular or particulate matter (including microbiological matter) on the surface or in the environment of interest, that can affect or degrade the relevant performance or life time
Cleanliness levels vs expected performance
Budgets to be defined and to be respected on ground and in flight
How to proceed?
© CNES
© CNES
© CNES
Consequences of molecular contamination
Degradation of thermal control surfaces
Performance loss of optical systems
Loss of electrical contact
Increase of internal pressure
migration of cleaning residues
Solder flux on connector
Porous materials for trapping and detection of space contaminants – CCMPP 2023

## Slide 4: Trapping
Low P
Charcoal
Mesoporous silica
Porous alumina
Zeolites
Conventional methods for contamination mitigation:
Bake-out of the payload / platform
Low outgassing materials
Specific design
Venting holes
© CNES
Porous materials for trapping and detection of space contaminants – CCMPP 2023
Expensive and time-consuming
Limited effectivness
Other solution: trapping of contaminants
Use of molecular adsorbent
X
Tetrahedra TO4
T = SiIV, AlIII
H. Kirsch, control of molecular contamination by adsorption on porous solids, PhD UHA – CNES, 2005

## Slide 5: Trapping
Porous materials for trapping and detection of space contaminants – CCMPP 2023
H. Kirsch, control of molecular contamination by adsorption on porous solids, PhD UHA – CNES, 2005
How to choose the right zeolite?
Selection of zeolite (nature, Si/Al molar ratio…) to adsorb a specific contaminant
Molecule per cell
Pressure (Pa)
Molecule per cell
Pressure (Pa)
Simulation
µVT ensemble. One Monte Carlo step  translation or rotation of molecules
Used for the study of liquid-vapor stability + calcul of vapor pressure
Adsorbate-adsorbate / intramolecular / adsorbate-adsorbent interactions
Cristallographic models  Fitch, Mortier and Olson  structure, cell coordinates, cations location…
Cyclohexane adsorption in silicalite-1
Dcyclohexane > Dpores
 Channel intersections

## Slide 6: Trapping
Porous materials for trapping and detection of space contaminants – CCMPP 2023
How to use it in satellite ? Powder  risk of particulate contamination
#1: Films (IS2M/CNES)
SEM images of (a) the EMC-1 top layer surface after hydrothermal treatment on seeded substrate and (b) the thickness of the ZSM-5 and EMC-1 bi-layer film
Scheme representing the overall method for the synthesis of a bi-layer film
n-hexane adsorption isotherms at 25 °C of the ZSM-5 bottom layer (square) and the ZSM-5 and EMC-1 bi-layer film (triangle)
Films with several zeolites = wider range of molecules to be trapped
T. J. Daou, N. Lauridant, G. Arnold, L. Josien, D. Faye, J. Patarin, Synthesis of MFI/EMT zeolite bi-layer films for molecular decontamination, Chemical Engineering Journal, Vol. 234, 2013, 66-73
N. Lauridant, T.J. Daou, G. Arnold, H. Nouali, J. Patarin, D. Faye, Zeolite hybrid films for space decontamination, Microporous and Mesoporous Materials, Vol. 172, 2013, 36-43
N. Lauridant, T. J. Daou, G. Arnold, M. Soulard, H. Nouali, J. Patarin, D. Faye, Key steps influencing the formation of ZSM-5 films on aluminum substrates, Microporous and Mesoporous Materials, Vol. 152, 2012, 1-8
N. Lauridant, T. Jean Daou, Gilles Arnold, Joël Patarin, Delphine Faye, MFI/∗BEA hybrid coating on aluminum alloys, Microporous and Mesoporous Materials, Vol. 166, 2013, 79-85

## Slide 7: Trapping
Porous materials for trapping and detection of space contaminants – CCMPP 2023
G. Rioland, T. J. Daou, D. Faye, J. Patarin, A new generation of MFI-type zeolite pellets with very high mechanical performance for space decontamination, Microporous and Mesoporous Materials, Vol. 221, 2016, 167-174
G. Rioland, P. Dutournié, D. Faye, T. J. Daou, J. Patarin, Prediction of the mechanical properties of zeolite pellets for aerospace molecular decontamination applications, Beilstein Journal of Nanotechnology, Vol. 7, 2016, 1761-1771
G. Rioland, H. Nouali, T. J. Daou, D. Faye, J. Patarin, Adsorption of volatile organic compounds in composite zeolite pellets for space decontamination, Adsorption, Vol. 23, 2017, 395-403
S. Maurice, R.C. Wiens, P. Bernardi, P. et al. The SuperCam Instrument Suite on the Mars 2020 Rover: Science Objectives and Mast-Unit Description. Space Sci Rev Vol. 217, 2021, 47
D. Faye, A. Jakob, M. Soulard, P. Berlioz, Zeolite adsorbers for molecular contamination control in spacecraft, Proc. of SPIE Vol. 7794, 2010, 77940B-1
How to use it in satellite ?
#2: Pellets (IS2M/CNES)
SEM images of the interactions between MFI-type zeolite and sodium silicate
Hydraulic press used for the shaping of powder
n-hexane adsorption isotherms at 25 °C for different formulations
Pellets with several zeolites = wider range of molecules to be trapped
Chemcam/Supercam laser cavity

## Slide 8: Trapping
Porous materials for trapping and detection of space contaminants – CCMPP 2023
Solide line = pressure profile during an adsorption test under a constant water vapor flow at RT
Dashed line = pressure without getter
Hatched area = the 14-months SEIS-equivalent time
Dotted line = pressure budget allocation
Different views (a,b,c) of the central getter assembly, and the development getter (d) unit adjacent to a ZLA composite molded in the canister shape
How to use it in satellite ?
#3: Aerogel (JPL/CNES)
Flight instrument plate with assembled getters
M.P. Petkov, S.M. Jone, G.E. Voecks et al. Development of the Primary Sorption Pump for the SEIS Seismometer of the InSight Mission to Mars. Space Sci Rev, Vol. 214, 2018, 112
SEIS instrument (InSight Mars lander) worked very well: detection of quakes on Mars

## Slide 9: Trapping
Porous materials for trapping and detection of space contaminants – CCMPP 2023
M. Diboune, H. Nouali, M. Soulard, J. Patarin, G. Rioland, D. Faye, T. J. Daou, Black zeolite coatings for stray light reduction and in-orbit molecular decontamination, Microporous Mesoporous Mater., Vol. 359, 2023, 112654
M. Diboune, H. Nouali, M. Soulard, J. Patarin, G. Rioland, D. Faye, T. J. Daou, Efficient Removal of Volatile Organic Compounds by FAU-Type Zeolite Coatings. Molecules Vol. 25, 2020, 3336.
M. Diboune, H. Nouali, M. Soulard, J. Patarin, G. Rioland, D. Faye, T. J. Daou, Green hybrid zeolite coatings for on-orbit molecular decontamination, Microporous and Mesoporous Materials, Vol. 307, 2020, 110478,
How to use it in satellite ?
#4: Paints (IS2M/CNES)
SEM images of a zeolite paint based on a mixture of commercial binders + zeolite + solvent
N2 adsorption isotherms at 77 K of different paint formulations
Final result  addition of black pigment for straylight
Paints used in vacuum chamber (bake-out, TVAC…) to protect sensitive surfaces

## Slide 10: Detection
Sorption features
Optimal affinity
Reversible sorption isotherm
Selectivity
Fast sorption kinetics
Material metrics
Thermal stability
Film processability
Environmental friendly
Commercial availability
Metal-Organic Frameworks (MOFs)
Variety of pore size / shape + functionalization
MOF@QCM as gases and Volatile Organic Compounds (VOCs) sensors: COx, NOx, NH3, H2S, SOx, BTEX, alcohols, alkanes…
No MOF-based sensors for siloxane detection
Porous materials for trapping and detection of space contaminants – CCMPP 2023
Nature of contaminants: RGA, wipe, witness sample … delay, multi-steps, uncertainty, operator dependent, location…
Need to track in situ and in real-time the nature of contaminant deposit
Sensitive porous sorbent deposited as a layer on QCM

## Slide 11: Detection
  IUPAC 20131: “A Metal-Organic Framework, abbreviated to MOF, is a Coordination Network with organic ligands containing potential voids.” “A coordination entity is an ion or neutral molecule that is composed of a central atom, usually that of a metal, to which is attached a surrounding array of atoms or groups of atoms, each of which is called a ligand”
Pure Appl. Chem., 2013, 85, 8, 1715
A. Gutiérrez-Serpa, I. Pacheco-Fernández, J. Pasán, V. Pino, Metal–Organic Frameworks as Key Materials for Solid-Phase Microextraction Devices-A Review. Separations Vol. 6, 2019, 47
  Cristallographic database:
  30 000 MOFs
  Simulation:
  130 000 MOFs
Porous materials for trapping and detection of space contaminants – CCMPP 2023
Notes: “A coordination compound extending, through repeating coordination entities, in 1 dimension, but with cross-links between two or more individual chains, loops or spiro-links, or a coordination compound extending through repeating coordination entities in 2 or 3 dimensions.”

## Slide 12: Detection
Best MOF for D4 capture: PCN-777
Best MOF for D4 sensing: MIL-101 (Cr)
D4, Si4O4(CH3)8
Porous materials for trapping and detection of space contaminants – CCMPP 2023

## Slide 13: Detection
13
MIL-101(Cr)@QCM
Spin coating deposition
mMIL-101(Cr) = 20-40 μg
F0 = 10 MHz
EtOH suspension (ILV)
Optical images
XRD
Porous materials for trapping and detection of space contaminants – CCMPP 2023
MOF deposition
Notes: For the preparation of a film of MIL-101(Cr), a colloidal suspension of MIL-101(Cr) NPs was prepared in ethanol at a concentration of 30 g / L. The MIL-101(Cr) nanoparticle film was prepared through the deposition of 50 μL of this colloidal solution by spin coating at a spinning speed of 2000 rpm for 60 s. The film was then air-dried at ambient temperature.

## Slide 14: Adsorption: DVS
Note : Calibration is required to identify the exact partial pressure of D4 in the carrier gas using a reference material
Porous materials for trapping and detection of space contaminants – CCMPP 2023
Detection
Notes: The pressure inside the balance chamber is dynamically adjusted, using a mass flow controller on the inlet side and a butterfly valve on the outlet side that is connected to a vacuum system. Combined with the low-pressure vacuum control of the DVS, which can maintain a total pressure down to 1 Pa, minute concentrations of D4 can be achieved, corresponding to 4 × 10−4 Pa, and equivalent to 40 ppb or 30 μg m−3 at 1 bar and 303 K (30 °C

## Slide 15: MIL-101(Cr)@QCM for D4 sensing
Good repeatability
Full reversibility
Full regeneration (vacuum / 303 K)
Blank QCM = Negligible response
LOD < 40 ppb
High sensitivity = 1000 & 3000 Hz log10(ppm)-1
E. Gulcay, P. Iacomi, G. Rioland, G. Maurin, S. Devautour-Vinot, Airborne toluene detection using Metal-Organic Frameworks, ACS Appl. Mater. Interfaces, Vol. 14, 2022, 48, 53777
P. Iacomi, E. Gulcay, P. Pires Conti, S. Biswas, N. Steunou, G. Maurin, G. Rioland, S. Devautour-Vinot, MIL-101(Cr) MOF as an effective siloxane sensor, ACS Appl. Mater. Interfaces, Vol. 14, 2022, 15, 17531
E. Gulcay, P. Iacomi, Y. Ko, J.-S. Chang, G. Rioland, S. Devautour-Vinot, G. Maurin, Breaking the upper bound of siloxane uptake: metal–organic frameworks as an adsorbent platform, J. Mater. Chem. A, Vol. 9, 2021, 12711
Porous materials for trapping and detection of space contaminants – CCMPP 2023
Detection

## Slide 16: Conclusion
Trapping:
Zeolite ➙ suitable for numerous contaminants
  Low vapour pressure adsorption
  Customize cations, Si/Al molar ratio…
  Shapes
Ongoing work
  Flight experiment  detection and trapping
  Tests in vacuum chamber
Detection:
MOF selection ➙ high-throughput computational screening (HTCS)
  Geometry, energy, hydrophobicity
MIL-101(Cr)@QCM ➙ suitable for D4 sensing
  Reversibility, sensitivity, repeatability, fast response / recovery times
Ongoing work
  Flight experiment  detection and trapping
  Tests in vacuum chamber and cleanroom
  Other molecules (phthalate, toluene…)
  Surface elastic wave components
Porous materials for trapping and detection of space contaminants – CCMPP 2023

## Slide 17: Thank you!
CCMPP-2023